Реферат
Конончук О.П.

Ковальчук Я.О.

Реферат
Дубіжаський Д.І.
Н. Контр.

  Консультант
№док.

Арк.
Кільк.
Стадія

Аркушів
Аркуш

ТНТУ, гр. МБм-61

Підпис
Дата

ДРМ 164.00.00.000 ПЗ

Зм.

Розробив
Перевірив
Затвердив
Дубіжаський Д.І.

  Пошва А.В.
Актуальність теми. Методи неруйнівного контролю міцності бетону широко застосовуються для діагностики технічного стану бетонних і залізобетонних конструкцій з певним терміном експлуатації, а також контролю якості зведених конструкцій. Метод ультразвукового контролю міцності бетону є одним з ефективних, в порівнянні з іншими неруйнівними методами, оскільки він дозволяє оцінити міцності не тільки поверхневого шару бетону, а й інтегральні параметри міцності.
Прийняті основні рішення інженерної частини дипломної роботи:
- в архітектурно-будівельному розділі подано коротку характеристику реконструкції офісного центру;
- в розрахунково-конструктивному розділі проведено розрахунок збірниx залізобетонниx елементів каркасу (багатопустотної плити перекриття, та сходового маршу);
 - в розділі теxнологія та організація будівельного виробництва розроблено календарний план виконання робіт по реконструкції і бедгенплан.
Мета роботи. Метою експериментальних досліджень є оцінювання точності вимірювання міцності бетону дослідних зразків ультразвуковим методом неруйнівного контролю та побудова градуювальних залежностей.
Завдання роботи:
        - провести огляд технічної літератури за темою дослідження;
- розробити програму та методику експериментальних досліджень;
- провести експериментальне дослідження дослідних зразків
ультразвуковим методом неруйнівного контролю, з паралельним випробуванням руйнівного методу на стиск;
- виконати статистичну обробку даних та проаналізувати результати експериментальних досліджень;

- побудувати градуювальну залежність і оцінити її достовірність.

Арк.

ДРМ 164.00.00.000 ПЗ

Галузь застосування. Будівництво, обстеження, ремонт та реконструкція будівель і споруд.
Об’єкт дослідження. Куби і залізобетонні плити.
Предмет дослідження. Кубова міцність бетону ультразвуковим методом.
Методи дослідження. Аналіз літературних джерел; аналіз експериментальних досліджень, аналіз експерементальних досліджень за спеціально розробленою методикою.
        Наукова новизна проведених досліджень:
        – розроблено програму та проведено експериментальні дослідження міцності бетону методом неруйнівного та руйнівного контролю;
        – отримано нові дані експериментальних досліджень міцності бетонів різних класів ультразвуковим методом;
        – проаналізовано отримані дані та побудовано градуювальну залежність.
        Взаємозв’язок з іншими роботами. Дана робота проводилася в комплексі з експериментальними дослідженнями неруйнівного контролю міцності бетону студентами групи МБм-61 Муканом В.І., Павлик Т.Р., Стрільчуком Д.В., Василиною В.В., Василиною Ю.А.
Ключові слова: міцність, неруйнівний контроль, бетон, градуювальна залежність, ультразвуковий метод.
Обсяг та структура роботи. Дипломна робота складається зі вступу, 8 розділів, висновків та списку використаних джерел із 57 найменувань. Робота викладена на 144 сторінках, із них 140 сторінки основного тексту, 4 сторінок списку використаних джерел, 28 таблиць та 60 рисунки.
Публікації. Результати роботи опубліковані у збірнику тез:Аналіз кубової міцності бетону неруйнівними методами контролю/ Т.Р.Павлик, В.І.Мукан, А.В. Пошва //VIІ Всеукраїнська студентська науково-технічна конференція "ПРИРОДНИЧІ ТА ГУМАНІТАРНІ НАУКИ. АКТУАЛЬНІ ПИТАННЯ", (Тернопіль, 24–25квітня 2014.) / М-во освіти і науки України, Терн. націон. техн. ун-т ім. І. Пулюя [та ін]. – Тернопіль: ТНТУ, 2014. – с. 232.
        Summary
        Actuality. Methods of nondestructive testing of concrete strength are widely used for the diagnosis of technical condition of concrete and reinforced concrete structures of certain lifetime and quality control erected structures.The ultrasonics trength testing method of concrete is effective, compared with other non-destructive methods, because it is a measure of the strength characteristics of not only the surface layer of concrete, but also integrated strength parameters.
        Accepted engineering major decisions of the thesis:

Арк.

ДРМ 164.00.00.000 ПЗ

 - In the architectural and construction section gives a brief description of office rehabilitation center;
 - In to calculation-structural section the calculation of collapsible reinforce-concrete elements framework is conducted (core slabs, and a flight of stairs);
 - In a section technology and organization of a build production the calendar plan of implementation of works is developed for reconstructions and budgenplan.
        Purpose. The objective of experimental studies is to evaluate the accuracy of measuring the strength of concrete test samples by ultrasonic non-destructive testing and building individual calibration dependencies.
        Tasks:
  -Review the technical literature on this particular research;
- Develop a method and program for experimental studies;
- conduct experimental research prototypes by ultrasonic nondestructive testing,
parallel testing method destructive compression;
- Perform statistical processing and analysis of experimental results;
-Analysis of the data and constructed calibration dependence.
        Field of application. The examination, diagnosis, repair and reconstruction of buildings.
        The object of study. Concrete cubes and slabs.
       Subject of the study. The strength of concrete measured by the ultrasonic method.
       Methods. Analysis of the literature; analysis of experimental studies, analysis of theoretical studies on developing a new technique of measuring the strength of concrete.
       New scientific developments on the research.

Арк.

ДРМ 164.00.00.000 ПЗ

- A program conducted for experimental research on the strength of concrete using ultrasonic non-destructive testing;
- New data of experimental research on the strength of different types of concreteusing the ultrasonic method;
 - Analyzed the data and found satisfactory convergence between non-destructive and destructive methods of testing concrete strenght.
        Interconnection with other robots. This work was carried out in conjunction with experimental studies of non-destructive testing of concrete strength by students of MBM-61 Mukan VI, Pavlik TR, Strilchuk DV, Vasilina VV, Vasilina YA.
       Tags: strength, non-destructive testing, concrete, calibration dependence ultrasonic method.
       The scope and structure of the work. Thesis consists of an introduction, 8 chapters, conclusions and list of sources of 57 items. The work described in 145 pages, including 140 pages of main text, a list containing 2 pages of used sources, 30 tables and 51 figures.
       Publications. The results were published in the book of abstracts: Analysis vat of concrete strength by non-destructive methods of control / TR Pavlik, VI Mukan, AV Poshva // VII All-Ukrainian Student Scientific Conference "sciences and humanities. TOPICAL ISSUES" (Ternopil, 24 - 25 April 2014) / Ministry of Education and Science of Ukraine, Tern. NA. Sc. University of them. Pul'uj I. [and others]. - : TNTU,
2014. - p. 232.